Shielding Paint for protection from electromagnetic energy

One of these revolutionary paints contains carbon as the exclusive conducting element therefore it will not corrode and has long-term durability. The second uses silver to gain an even higher reduction in electromagnetic energy.

Shielding paints – the revolution in shielding technology.
One of the top selling products for electromagnetic shielding is the metal free high frequency shielding paint. It is applied like any other paint. Most of these paints are suited for both indoor and outdoor use. There are different qualities. I have included two of the several available.

These paints are suitable for a wide range of applications.
Living areas: Protection from HF-radiation from cellphone towers, TV and radio broadcasting antennas, radar, digital standard cordeless telephones, wireless networks and other last-mile applications. To prevent data-stealing from wireless networks, to prevent interception of potentially bugged conference rooms, to shield EMI-sensitive facilities and equipment. Medicine: Protection of sensitive technical equipment. Further applications: schools, nurseries, hotel rooms, hospital rooms, recording studios, etc.

(Pure acrylic, HF radiation + LF electric €elds, Interior + Exterior application)
This paint has a high attenuation even with a single coat. Attenuation of 36 dB (shielding effectiveness of 99.98 %) at typical coverage in one coat, attenuation of 43 dB (shielding effectiveness of 99.995 %) at typical coverage with two coats. This paint has good adhesion on most interior surfaces, such as old emulsion paint layers(regular interior pain latex or vinyl, sheetrock, cement, plaster, masonry, wood, etc. Also, it can easily be covered with water based latex or vinyl paint, the color is black. This paint is reinforced with long conductive fibers, which bridges the gap in the underground. This simplifies the process so no ground strip is needed, especially in outdoor applications. Highly breathable, free of solvents, plasticisers, etc

(Acrylic, HF radiation + LF electric €elds, Interior + Exterior application)
This is the newer paint for interior and exterior applications. It has pure silver as the sole conductive component. This product has an extremely high attenuation, which is up to 50 dB (shielding effectiveness of 99.999 %) in one layer. This paint has a hard and mechanically resilient surface. Excellent adhesion on many interior and exterior surfaces and substrates like old emulsion paint layers, sheetrock, cement, plaster, masonry, wood, plastics, etc. It also can be easily be covered with water based emulsion paint (also known as latex or vinyl paint). To bridge forming gaps in the underground, it is recommend that you use a grounding-strap EB. Information on this product is on this Web site. Use of this product usually increases the effectiveness of the paints. Low VOC content, highly breathable, free of solvents, plasticisers, etc.

Ground connection set for shielding paints
	
Ground strap

Ground connection set is specifically designed to ensure proper grounding of the shielded paint. For each connected area (or surface) of shielding paint coat one grounded connection set is required. It is a high grade steel plate 8x8x.03cm with conductive fleece backside. It comes with 4 stainless steel screws, 4 dowel / wall plugs 6mm, 1meter grounding cable.

 

	

It is very easy to do, the tape is a self-adhesive strip that comes in roll and it is painted over. You attach it along the bottom of the wall all the way around the room. Then you run one strip from the bottom of one wall up to the ceiling across the ceiling and down to the bottom of the other wall. All areas / surfaces painted with shielded paint need to be grounded for safety and maximum attenuation. In the event there is a crack in the wall the tape will ensure grounding. The self adhesive strap is made with highly conductive silver containing glue; 100% corrosion resistant copper strap, and is tin coated on both sides. It is 2 cm thick and is 10 meters long.